NOVOFLEX | Cab-Lok Non-Returnable Cable Ties

In critical installations, slippage or loosening is not acceptable. Fastening systems must deliver permanent, high-strength locking that remains stable under load and environmental exposure.

Novoflex Cab-Lok Non-Returnable Cable Ties are engineered from UL-listed Nylon 6.6 with a precision locking head mechanism that ensures a secure, one-way ratchet action. Once tightened, the tie cannot loosen or reopen, providing dependable long-term fastening across electrical, industrial, and infrastructure applications.

Designed for high tensile strength and environmental resistance, these ties deliver consistent performance where security and reliability are critical.

Key Features

- Non-Returnable Locking Mechanism
One-way ratchet design ensures permanent fastening; removal requires cutting.

- High Tensile Strength
Engineered to withstand loads up to 105 kg (variant-dependent).

- Material: UL-Listed Nylon 6.6
Provides durability, mechanical strength, and long-term stability.

- Flammability Rating
Complies with UL94 V-2 standards.

- Environmental Resistance
Resistant to fungi, corrosion, and most acids.

- Temperature Performance

  - Continuous: -25°C to +85°C

  - Intermittent: up to +105°C (500 hours)

- Colour Options
Standard: Natural White & UV Black
Custom: Red, Yellow, Blue, Green (MOQ applicable)

Where It Performs Best

- Electrical & Industrial Cable Bundling

- Wiring Harness & Panel Assembly

- Infrastructure & Construction Installations

- Outdoor Applications (UV Black variant)

- Applications requiring tamper-resistant fastening

Positioning Clarity

- Use when:

  - Permanent, non-releasable fastening is required

  - High tensile strength is critical

  - Long-term reliability under load is essential

- Avoid when:

  - Reusability or frequent adjustments are needed

  - Temporary bundling is required

Standards & Compliance

- Low Smoke Test: ASTM E662 compliant

- Oxygen Index: 28 (BS ISO 4589)

- Burning Fume Toxicity: Meets BSS 7239 requirements

Packaging

- Miniature: 1000 pcs

- Intermediate / Standard / Heavy Duty: 100 pcs

Why Novoflex

In fastening systems, failure often begins at the locking point.

Novoflex Cab-Lok ties ensure consistent locking integrity, high load resistance, and zero slippage, even under demanding conditions.